3.2V 30Ah

Lithium Iron Phosphate (LiFePO4) Battery

Product Features

Model:HZF-3.2-30-SA

Safest LiFePo4

cells for safe use no ﬁre no explosion

Long Life Cycles

>2000 cycles@0.2C,Charge/Discharge at 100%DOD

Powerful Energy

Quick charging,high quality and high discharge rate lithium battery cells providing more energy.

Built-in intelligent BMS

Over Charge /Discharge voltage and current protection, Short circuit protection ,Over temperature protection.

Clean Energy

HuaZhen Lithium Battery are the ultimate ,No toxic material ,No Pb.

Kg

2

Light Weight

about 40%~50%of the weight of SLA battery

Replacement

Replacement for SLA battery with compatible Housing

Customized

Battery Voltage,Capacity,Current,Size ect all can be customized to meet speciﬁc applications

Model #: HW-12.8V-9Ah

| Electrical Characteristics | Technology | Lithium Iron Phosphate |
| --- | --- | --- |
|  | Nominal Voltage | 3.65V |
|  | Nominal Capacity | 30Ah± 5%@0.2C |
|  | Energy | 384Wh |
|  | Cycle Life | 100% Depth of Discharge ~2000 cycles |
|  | Internal Resistance | 30mΩ |
|  | Self Discharge | ＜3% per month @25℃ |
| Charge | Charge mode | CC&CV(0.2C Constant current & 3.65V Constant voltage@0.02C) |
|  | Max. Charge Voltage | 3.65V |
|  | Standard Charge Current | 6A |
|  | Max.Charge Current | 15A |
| Discharge | Discharge Cut-oﬀ Voltage | 2.5V |
|  | Standard Discharge Current | 15A |
|  | Max.Continuous Discharge Current | 30A |
|  | Pulse Current | / |
| Operating Condition | Storage Temperature | 0℃to45℃(32℉to113℉) |
|  | Humidity | 60±25% |
|  | Charge Temperature | 0℃ to 45℃(32℉to113℉) |
|  | DischargeTemperature | -20℃to 45℃(32℉to113℉) |
| Structure | Water Dust Resistance | / |
|  | Teminal | / |
|  | Carrying | / |
|  | Case and Cover | PVC |
|  | Dimension（L*W*H) | 177*72*34mm |
|  | Weight | Approx1000g |

Product Description

2

Years limited

Diﬀerent DOD Discharge Cycle Life Curve @0.5C, 25℃

Diﬀerent Rate Discharge Curve @ 25℃

110%

Remaining capacty(%)

100%

90%

80%

70%

60%

| 100%DOD 80%DOD 50%DOD |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |

0	1000 2000 3000 4000 5000 6000 7000

Numenber of Cycles

14.0

13.5

13.0

Voltage(V)

12.5

12.0

11.5

11.0

10.5

10.0

| 0.2C 0.5C 1C |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |

0%	20%	40%	60%	80%	100%

Capacity(%)

Address: No.1 Huaxiang Road, Xingtai Development Zone, Changtai, Zhangzhou, Fujian, China, 363900.

E-mail: hxpower@huaxiangbattery.com http://www.huaxiangbattery.com Tel://+86-0596-8369885