Specifications

| Nominal Voltage |  |  | 12 V |
| --- | --- | --- | --- |
| Capacity(10HR, 25℃) |  |  | 8Ah |
| Dimension | Length |  | 150±2mm (5.91inch) |
|  | Width |  | 86±2mm (3.39inch) |
|  | Height |  | 105±2mm (4.13inch) |
| Approx. Weight |  |  | 2.15kg (4.74lbs)±5% |
| Approx.ACID Per Battery |  |  | 0.444 L |
| Charge Current (A |  |  | 0.8A（14.4V constant voltage charge) |
| Operating temperature range |  |  | -20℃～50℃ (-4℉～122℉) |
| Standard Charging method (25℃) | Current |  | 0.8 |
|  | Time |  | 5~10h |
| Quickly Charging method (25℃) | Current |  | 4.0A |
|  | Time |  | 1h |
| Cold Cranking Amperes(-18℃) |  |  | 90 A |
| Charge Retention (self-discharge life ) at 20℃ (68℉) |  | 3 month | 80% |
|  |  | 6 month | 75% |
| Warranty |  |  | 1year |
| Case Material |  |  | PP |

Discharge Characteristics(25℃)

Dimensions

Terminal